Table of contents
TECEfloor
TECEfloor
TECEfloor dry-wall panel TP 30/16 BMB
Pipe base panel for installation of
underfloor heating according to
construction type B (laying pipe within
the insulation layer under screed).
Allows use with standard dry screed
elements (Knauf, Fermacell, Rigips,
etc.) as well as wet screed (cement
screed, flow screed). Made from expanded
polystyrene hard foam (EPS), with pipe
layout channels for incorporating
TECEfloor heat conduction profiles and
TECEfloor underfloor heating pipes 16 x
2 mm. Can be laid in single and double
meander, HBCD-free.
Material: expanded polystyrene (EPS 035
DEO), building material class E
Thermal conductivity: 0.035 W/mK, R=
0.77 m²K/W
Compression strength 150 kPa at 10 %
compression in accordance with EN 826
Spacing: VA 150, VA 300 (single and
double meander)
Dimensions (L x W x H): 1150 x 750 x 30
mm
BMB at TECE stands for products based on
the biomass balance approach. Here,
biogenic raw materials (waste and
residual materials from biomass) are
used together with fossil raw materials
in the manufacture of basic chemical
products in the production network. The
bio content is then mathematically
allocated to the TECEfloor TP 30/16 BMB
dry construction boards on the basis of
the REDcert² certification system.
BMB products have the same quality as
non-BMB products, as the formulation of
the product is identical to that of the
fossil equivalent. TECE’s biomass
balance approach supports the use of
biogenic raw materials, which leads to
savings in fossil raw materials and a
reduction in greenhouse gas emissions.
Order No.: 77520009